Kedel Limited

Kedel Limited

Daisy Mill ( Gate 3 )

Daisy Street

Waterside

Colne

Lancashire

BB8 8ER

Report Reference: 1102IPLA180510

Purchase Order: n/a

Grip Potential Ltd 0845 163 0 163 info@grip-potential.com www.grip-potential.com

Company No: 6783045 Registered Address: Ringstead Business Centre, 1-3 Spencer Street, NN14 4BX

Report Reference: 1102IPLA180510 1 of 8

Page

Reported results in no way imply that the flooring under test is approved or endorsed by

Grip Potential Ltd. Grip Potential Ltd do not give or assume warranty or condition, express

or implied, statutory or otherwise, as to condition, quality, performance, merchantability or

fitness for the purpose of the test subject and all such warranties and conditions are hereby

excluded save to the extent that such exclusion is absolutely prohibited by law. Grip

Potential Ltd shall not be liable for any subsequent loss or damage incurred by the client as

a result of information contained within this report. Results given herein refer only to areas

tested by Grip Potential Ltd.

Summary

Sample Slip Risk Comments

Low Test results indicate a low risk of slip in both

dry and water-wet conditions.

Plastic Decking

Report Reference: 1102IPLA180510 2 of 8

Page

Theory

The pendulum skid test forms the basis of the coefficient of dynamic friction measurement

of a floor. A calibrated ‘foot’ swings from a horizontal point of release, strikes the flooring

surface for a known distance, then reads the “pendulum test value” on its overswing. The

rubber slider that contacts the floor is constructed of ‘4S’ rubber (Standard Simulated Shoe

Sole) and is designed to replicate the most common slipping motion experienced by

pedestrians wearing shoes. A softer, more malleable, rubber (TRL rubber) may be used to

simulate a barefoot or casual shoe slip. Pendulum testing is one of the few methods that

models the formation of a hydrodynamic squeeze film between the floor and shoe sole, a

major factor in a wet slip.

Research carried out by the Health and Safety Laboratory, in conjunction with the UK Slip

Resistance Group (UKSRG), has shown that it is possible to assess the characteristics of

floor surface materials needed for satisfactory slip resistance. The Health and Safety

Laboratory has developed a “reliable and robust” test method that forms the basis of Grip

Potential’s assessment procedure.

A surface roughness meter is used to measure the ability of the floor’s surface to puncture

the hydrodynamic squeeze film. The film forms a barrier between sole and floor and

significantly reduces grip, in the same way that a car tyre aquaplanes. The minimum

recommended valley to peak height for a water wet surface is 20μm. A thicker

contaminant, such as motor oil, will require a much greater surface roughness in order to

facilitate a sole-floor contact. For this reason it is important to take into account expected

contaminants when specifying a floor surface.

A site assessment is an important component in determining the slip risk of any given floor.

The HSE’s pedestrian slip potential model highlights important environmental factors in a

slip. Contaminating substances, frequency and methods of cleaning, types of footwear and

likely pedestrian behaviour all affect the potential for a slip incident and are given due

consideration.

Report Reference: 1102IPLA180510 3 of 8

Page

Method

BS 7976-2:2002 - Pendulum Testers, Method of Operation

PTV

<25

25-35

>35

Table 1. Slip Potential classifications from Pendulum Test Values

High

Slip Potential

Coefficient of dynamic friction measurement is carried out in accordance with BS 7976 and

the UKSRG Guidelines 2005. These industry standard methods of testing are essentially the

same but with a slight difference between the two methods of preparation of the rubber

sliders. Testing has been carried out in accordance with the UKSRG Guidelines 2005 as

both the HSE and UKSRG agree that this is best practice.

A prepared standard rubber slider attached to a weighted 'shoe' is allowed to swing from a

horizontal point of release. The slider is mounted on a spring loaded bracket and makes

contact with the floor for a known distance. The height to which the shoe travels after

contacting the floor gives a reading of the Pendulum Test Value (PTV, formally known as

SRV Slip Resistance Value). The dynamic coefficient of friction of a test surface has a direct

and measurable effect on the PTV reading obtained.

Test surfaces are subject to eight measurements of the PTV with the first three being

discounted from calculations of the mean. Tests are carried out in the principal direction, at

45° to the principal direction and at 90° to the principal direction. Each direction is tested

under both wet and dry conditions, totalling 48 measurements. A mean value is generated

for wet and dry tests based on the performance in different directions. A slip potential

classification can then be applied using the following table from the UKSRG Guidelines.

Moderate

Low

Surface Roughness Measurement (Rz)

Rz (μm)

<10

10-20

>20

Table 2. Slip Potential classifications from surface roughness (Rz) values

Report Reference: 1102IPLA180510 4 of 8

High

Low

Surface roughness can be used to give a general indication of the slip risk potential of a

floor, though it is by no means a comprehensive test. Grip Potential use surface roughness

measurements married to pendulum results to enable accurate ongoing monitoring of the

surface. The UKSRG published the data shown in the table below to use in conjunction

with pendulum testing.

Moderate

Page

Slip Potential

Surface roughness, in particular the Rz value, describes the ability of a floor to puncture the

hydrodynamic squeeze film. It is also a valuable tool to assess the wear level as over time

traffic will smooth a floor surface, changing its slip risk potential.

Grip Potential use a Surtronic Duo surface roughness meter for assessment. The meter

moves a stylus along the test surface, measuring the floor profile's average vertical peak to

valley distance in microns. A test site will be measured ten times using this method, with

tests carried out in random directions in an area local to the pendulum test. This is in line

with UKSRG guidelines.

Site Assessment

A Grip Potential site assessment aims to provide the client with all necessary information of

the factors contributing to slip risk of the tested areas. Drawing assessment criteria from a

wide range of expert sources ensures that a complete and thorough report of slip risk is

produced. Knowledge of factors adversely affecting slip risk allows intelligent decision

making in ongoing health and safety procedures.

A site assessment is designed to highlight factors that have an impact on slip risk potential.

The Grip Potential site assessment follows the pedestrian slip risk potential model as

developed by the HSE alongside guidance published by the UKSRG and CIRIA and our own

expert knowledge and experience.

Information required to complete the site assessment is gathered primarily at the time and

location of the test based on observations made by the test operator. Less obvious

information, such as cleaning regimes or shoe control measures, is supplied by the person

responsible for the site, or a representative of that person. Where information is uncertain,

or an assumption is made, it is made clear that this is the case.

Report Reference: 1102IPLA180510 5 of 8

Page

Test Equipment

Munro Portable Skid Tester

Notes:

Serial No: 0852

Calibrated by: BSI Product Services

Calibration date: 19/03/10

Certificate No: 3859

Calibration due: 19/03/11

Surface Roughness (Rz) Meter Calibration Plate

Notes:

Serial No: 112-2916

Calibrated by: GB Quality Assurance Ltd

Calibration date: 27/04/09

Certificate No: 55283

Calibration due: 27/04/14

4S Rubber Sliders (Slider #96)

Notes:

Batch No: 15306

Calibrated by: Munro Stanley London

Calibration date: 27/01/10

Certificate No: 63540

Disposal date: 27/01/11

TRRL Rubber Sliders (Slider #55)

Notes:

Batch No: 15377

Calibrated by: Munro Stanley London

Calibration checks are carried out regularly by way of

check testing on lapping film previously tested by a

UKAS accredited laboratory. Further to this, check

testing is conducted on site using lapping film and float

glass of a known value.

Sliders are prepared in line with guidance by the UKSRG.

Check testing is conducted both on lapping film

previously tested by a UKAS accredited laboratory and

float glass. This procedure is conducted prior to a site

visit and is in addition to the site check testing.

The Surtronic Duo surface roughness meter comes

equipped with a calibration plate of known roughness.

Prior to testing on site, check testing is carried out on

the calibrated plate.

Sliders are prepared in line with guidance by the UKSRG.

Check testing is conducted both on lapping film

Calibration date: 06/04/10

Certificate No: 63645

Disposal date: 30/03/11

Digital Level

Notes:

Serial No: 6029

Calibrated by: MD Calibration Services

Calibration date: 08/04/10

Certificate No: 121087

Calibration due: 08/04/11

Daily Check Test Values

Mean Expected

Lapping film: 64 64 64 63 63 64 63 ±1

Float glass: 8 8 8 8 7 8 5 to 10

Surface Roughness tested value: 21.5 μm

Surface roughness expected value: 21.5 μm

Report Reference: 1102IPLA180510 6 of 8

Page

PTV

previously tested by a UKAS accredited laboratory and

float glass. This procedure is conducted prior to a site

visit and is in addition to the site check testing.

The digital level is used to determine the gradient of the

test surface. The UKSRG give guidance on the effect a

slope has on the recommended minimum PTV.

Please note that all calibration certificates are available on request.

Test Results Plastic Decking

Test carried out by: Ben Powers Date of test: 21/05/10

Site location: Grip Potential Ltd Flooring type: Plastic

Substrate: n/a Application: Decking

Image 1. Test surface Image 2. Test surface

Pendulum Test Results Slider #96 (4S)

Direction Condition Mean

Principal 41 40 41 41 41 41

45° 43 43 42 42 42 42

90° 64 67 65 64 63 65

49

Principal 36 35 35 36 35 35

45° 37 37 37 37 37 37

90° 49 50 48 51 50 50

41

PTV

Dry

Mean wet PTV:

Mean dry PTV:

Wet

Pendulum test values indicate that slip risk potential in the dry is

Pendulum test values indicate that slip risk potential in the wet is

Surface Roughness (Rz) Results

Sample Rz (μm) Wet PTV: 35 Rz Value: 41.0

1 16.9

2 65.7

3 46.0

4 46.7

5 52.5

6 21.9

7 35.1

8 70.4

9 16.5 ≥ 42

10 38.1 < 42

Mean 41.0 < 29

Report Reference: 1102IPLA180510 7 of 8

Rz Value (μm) Indicative Slip Risk

Moderate

High

Assuming linear relationship between surface roughness

in microns and pendulum test values, the following can

be used as a guide when monitoring surface roughness

of the test surface.

Low

Low

The above results have been classified in accordance with the UKSRG Guidelines Issue 3,

November 2005.

Low

Surface roughness taken in the principal direction as this is the most slippery.

Page

Conclusion

Table 1. Results from various assessment measures employed

In the opinion of Grip Potential Ltd, the plastic decking sample under test demonstrated a

low risk of slip in dry conditions and a low risk of slip in water wet conditions.

The decking produced an average wet PTV over 3 directions in excess of 36, in accordance

with UKSRG guidelines this is classified as a "low slip risk". It should be noted that tests

conducted along the 'grain' produced a PTV of 35, which would be classified as a "moderate

slip risk". There is unlikely to be a significant difference in the number of falls a 35PTV

surface facilitates over a 36PTV surface. Surfaces exposed to water based contamination

should provide a low risk of slip in these conditions. The decking sample traversed parallel

to the 'grain' does not provide a low risk of slip.

Assuming an identical material composition, results suggest that the curvature of previously

tested samples was in fact providing favourable pendulum test results. The trough shape

may have been sufficiently great to provide an excess of pressure applied at the edges of

the slider. The same effect would not have been seen in a real slip with a rounded heel.

The flat samples tested above better represent the slip resistance that can be expected by

end users.

The common macro-profile decking design features deep grooves cut along the length of

the decking planks, as in the tested sample. This profile provides excellent grip at right

angles to the grain, with the profile effectively cutting through the fluid film lubricating a

Current risk management strategies n/a

Pendulum (BS 7976) in water wet conditions Low Slip Risk

Current Rz reading 41.0

Low Slip Risk

Estimated Rz threshold for low slip risk 42

Plastic Decking: Test Method Result

Pendulum (BS 7976) in dry conditions

Signed:

Ben Powers 24/05/10

Report Reference: 1102IPLA180510 8 of 8

slip. The slip resistance along the grain is compromised however, as the contact area is

reduced and there are no features cutting through the fluid film. In addition, the sample

under test featured a micro-profile similar to that of wood, running along the grain. A

directional micro-profile offers similar properties to a directional macro-profile. The ability

of the micro-profile to cut through the fluid film is significantly reduced along the 'grain'.

Page

The above assessment was carried out by Grip Potential adhering to the UKSRG, HSE and

CIRIA guidelines on pedestrian slip risk assessment. The results given are accurate

representations of data acquired on site and through the client. The results have been

interpreted to give slip risk classifications based on parameters recommended by the

UKSRG and HSE